**SECTION 08 17 43**

**SL Series Fire-Rated FRP Doors and Frames**

**PART 1 GENERAL**

1. **SECTION INCLUDES**
	1. SL-19-1FR Contemporary Wood Grain Fire-Rated Fiberglass Door.
	2. SL-19-1FR Contemporary Wood Grain Fire-Rated Fiberglass Door in Fire-Rated Metal Frame.
	3. SL-19-1FR Contemporary Wood Grain Fire-Rated Fiberglass Door in Fire-Rated Fiberglass Frame.
2. **RELATED SECTIONS**
	1. Section 04 00 00 – Masonry Mortar.
	2. Section 05 50 00 – Metal Fabrications.
	3. Section 08 01 17 – Operation and Maintenance of Integrated Door Opening Assemblies.
	4. Section 08 06 71 – Door Hardware Schedule.
	5. Section 08 06 80 – Glazing Schedule.
	6. Section 08 10 00 – Doors and Frames.
	7. Section 08 71 00 – Door Hardware.
	8. Section 08 80 00 – Glazing.
3. **REFRENCES**

* 1. [ASTM-D256](#ASTM_D_256) – Standard Test Methods for Determining the Pendulum Impact Resistance of Plastics.
	2. [ASTM-D570](#ASTM_D_570) – Standard Test Method for Water Absorption of Plastics.
	3. [ASTM-D638](#ASTM_D_638) – Standard Test Method for Tensile Properties of Plastics.
	4. [ASTM-D790](#ASTM_D_790) – Standard Test Methods for Flexural Properties of Unreinforced and Reinforced Plastics and Electrical Insulating Materials.
	5. [ASTM-D2583](#ASTM_D_2583) – Standard Test Method for Indentation Hardness of Rigid Plastics by Means of a Barcol Impressor.
	6. [ASTM D2794](https://www.astm.org/Standards/D2794.htm) – Standard Test Method for Resistance of Organic Coatings to the Effects of Rapid Deformation (Impact).
	7. [ASTM-E84](#ASTM_E_84) – Standard Test Method for Surface Burning Characteristics of Building Materials.
	8. [CAN / ULC S104](https://www.scc.ca/en/standardsdb/standards/25796) – Standard Method for Fire Tests of Door Assemblies.
	9. [UL 10B](https://standardscatalog.ul.com/standards/en/standard_10B_10) – Standard for Fire Tests of Door Assemblies.
	10. [UL 10C](https://standardscatalog.ul.com/standards/en/standard_10C) – Standard for Positive Pressure Fire Tests of Door Assemblies.
	11. [NFPA 80](https://www.nfpa.org/codes-and-standards/all-codes-and-standards/list-of-codes-and-standards/detail?code=80) – Standard for Fire Doors and Other Opening Protectives.
	12. [NFPA 252](https://www.nfpa.org/codes-and-standards/all-codes-and-standards/list-of-codes-and-standards/detail?code=252) – Fire Tests of Door Assemblies.
1. **SUBMITTALS**
	1. Must comply with Section 01 33 00 – Submittal Procedures.
	2. Action Submittals/ Informational Submittals.
		1. Product Data.
			1. Submit manufacturer’s product data sheets, catalog pages illustrating the products, description of materials, components, fabrication, finishes, installation instructions, and applicable test reports.
		2. Shop Drawings.
			1. Submit manufacturer’s shop drawings, including elevations, sections, and details indicating dimensions, tolerances, materials, fabrication, doors, panels, framing, hardware schedule, and finish.
		3. Samples.
			1. Submit manufacturer’s door sample composed of door face sheet, core, framing and finish.
			2. Submit manufacturer’s sample of standard colors for door face and frame.
		4. Testing and Evaluation Reports.
			1. Submit testing reports and evaluations provided by manufacturer conducted by and accredited independent testing agency certifying doors and frames comply with specified performance requirements listed in Section 2.01 C.
		5. Manufacturer Reports.
			1. Manufacturer’s Project References.
				1. Submit list of successfully completed projects including project name, location, name of architect, type, and quantity of doors manufactured.
	3. Closeout Submittals.
		1. Operation and Maintenance Manual.
			1. Submit manufacturer’s maintenance and cleaning instructions for doors and frames, including maintenance and operating instructions for hardware.
		2. Warranty Documentation.
			1. Submit manufacturer’s standard warranty.
2. **QUALITY ASSURANCE**
	1. Manufacturer’s Qualifications.
		1. Continuously engaged in manufacturing of doors of similar type to that specified, with a minimum of 25 years concurrent successful experience.
		2. Door and frame components must be fabricated by same manufacturer.
		3. Evidence of a documented complaint resolution quality management system.
3. **DELIVERY, STORAGE, AND HANDLING**
	1. Delivery.
		1. Deliver materials to site in manufacturer’s original, unopened, containers and packaging.
		2. Labels clearly identifying opening, door mark, and manufacturer.
	2. Storage.
		1. Store materials in a clean, dry area, indoors in accordance with manufacturer’s instructions.
	3. Handling.
		1. Protect materials and finish from damage during handling and installation.
4. **WARRANTY**
	1. Warrant doors, frames, and factory installed hardware against failure in materials and workmanship, including excessive deflection, faulty operation, defects in hardware installation, and deterioration of finish or construction in excess of normal weathering.
	2. Standard Period.
		1. Ten years starting on date of shipment.
	3. Limited lifetime
		1. Covers failure of corner joinery, core deterioration, and delamination or bubbling of door skin and corrosion of all-fiberglass products while the door is in its specified application in its original installation.
	4. Finish
		1. Stained SL-19-1FR face sheets: 5 years.
		2. Painted FR frames: 3 years.

**PART 2 PRODUCTS**

1. **FRP/ALUMINUM HYBRID DOORS**
	1. Manufacturer.
		1. Special-Lite, Inc.
			1. PO Box 6, Decatur, Michigan 49045.
			2. Toll Free (800) 821-6531, Phone (269) 423-7068, Fax (800) 423-7610.
			3. Web Site [www.special-lite.com](http://www.special-lite.com).
			4. E-Mail info@special-lite.com.
2. **DESCRIPTION**
	1. SL-19-1FR Contemporary Wood Grain Fire-Rated Fiberglass Door.
		1. Rated for 20 to 90 min maximum duration.
		2. Door Opening Size.
			1. 3’6” x 8’0” maximum size single swing.
			2. 7’0” x 8’0” maximum size standard pairs.
			3. Click or tap here to enter text.
		3. Construction.
			1. Door Thickness.
				1. 1-7/8” at door edge.
				2. Single Swing.

Hinge and lock stile, 2” minimum tectonite.

* + - * 1. Standard Pairs.

Hinge stile, 2” minimum tectonite.

Meeting edge, 3” minimum tectonite.

* + - 1. Rails.
				1. Top rail, 6” minimum tectonite.
				2. Bottom rail, 4” minimum for single swing, 4-1/2” minimum for pairs tectonite
			2. Core.
				1. WSCP-412 proprietary mineral core.
				2. 1-1/2” nominal thickness.
				3. 18 pcf minimum density.
			3. Face Sheet.
				1. Interior and Exterior.

0.120” thick, contemporary wood grain, stained FRP sheet.

Optional painted finish consult manufacturer.

* + - 1. Edge Channels.
				1. 0.062” thick, 3/4” leg, stainless steel edge channel.
				2. Applied to entire perimeter of the door.
				3. Sealed by 3M CP 25WB + Fire Barrier caulk applied to the inside edges of all the steel edge channels.
			2. Cutouts.
				1. Manufacture doors with cutouts for required vision lites per the manufactures listing.
			3. Hardware.
				1. Pre-machine doors in accordance with templates from specified hardware manufacturers.
				2. Field apply factory supplied gaskets and seals, full width intumescent and smoke seal required at top of door, smoke seals required on both jambs.
1. **FRAMING**
	1. Framing
		1. FR-Series Fiberglass Framing.
			1. Maximum of 45 min fire rating when installed in fiberglass frames.
			2. Materials.
				1. ¼” thick, solid, pultruded, FRP profiles.
				2. No corrosive components or reinforcements.
				3. Solid tectonite filler.
				4. No steel or aluminum filler is allowed.
			3. Perimeter Frame Members.
				1. Factory fabricated.
				2. Integral 5/8” x 2-1/4” doorstop.
				3. Mitered with 4” x 4” x 3/8” pultruded FRP angle reinforcement with interlocking pultruded FRP brackets.
				4. 5-3/4”, 6-3/4”, 7-3/4”, or 8-3/4” jamb depth.
				5. 2” face on jambs.
				6. 2” or 4” face on header.
				7. Knocked down for field assembly.
			4. Anchors
				1. Factory furnished as specified by drawings.
				2. Drywall tuck available.
		2. Any category C standard frame.
		3. Any category C proprietary frame.
2. **PERFORMANCE**
	1. Face Sheet.
		1. Standard Interior and Exterior Class A 0.120” thick, contemporary wood grain, painted FRP sheet.
			1. Surface Burning, ASTM-E84: Flame Spread ≤ 25, Smoke Developed ≤ 350.
	2. Door Assembly.
		1. 60 min pp category A door.
		2. 90 min pp category B door.
		3. 90 min pp category A door.
		4. Temperature rise @ 30 min, 250 °F when vision lites do not exceed 100 in².
		5. Temperature rise @ 60 min, 450 °F max.
3. **MATERIALS**
	1. Fiberglass.
		1. See 2.02.A.2.e.
		2. See 2.02.B.2.e.
		3. See 2.02.C.2.e
	2. Fasteners.
		1. All exposed fasteners will have a finish to match material being fastened.
		2. 410 stainless steel or other non-corrosive metal.
		3. Must be compatible with items being fastened.
4. **FABRICATION**
	1. Factory Assembly.
		1. Door and frame components from the same manufacturer.
		2. Required size for door and frame units, shall be as indicated on the drawings.
		3. Maintain continuity of line and accurate relation of planes and angles.
		4. Secure attachments and support at mechanical joints with hairline fit at contact surfaces.
	2. Shop Fabrication
		1. All shop fabrication to be completed in accordance with manufactures process work instructions.
		2. Quality control to be performed before leaving each department.
5. **FINISHES**
	1. Door.
		1. FRP Face Sheets
			1. Stained.
				1. [Color.](http://special-lite.com/wordpress/wp-content/uploads/files/Categories/Doors/Fiberglass%20Doors/Hybrid/Literature/SL-19-1-Color-Selections.pdf)

Choose an item.

* + - * 1. Custom colors available consult manufacturer.
	1. Frame
		1. Fiberglass.
			1. Two-part aliphatic polyurethane paint.
				1. [Color.](https://special-lite.com/product/fr-series-framing/)

Choose an item.

* + - * 1. Custom colors available consult manufacturer.
				2. Unique, high-solids, high-build, multifunctional coating.
				3. Low VOC, high-gloss, self-priming coating.
				4. Impact Resistance, ASTM-D2794: 140 in·lbs (direct), 50 in·lbs (reverse) @ 5 mils thickness.
				5. Taber Abrasion, 1 kg load, 1000 cycles, CS-17 wheel: 60.2 mg.
				6. Graffiti cleaning with Amerase with gloss retention: 100 cycles.
				7. Chemical Resistance.

Excellent.

Acidic.

Alkaline.

Salt Solutions.

Seawater.

Fresh Water.

Petroleum Products.

1. **ACCESSORIES**
	1. Vision Lites.
		1. Factory Glazing.
		2. Stainless Steel vison kit with 3/16” NGP Firelite NT, clear.
		3. Size as indicated on the drawings.
		4. 60 to 90-minute rated doors.
			1. Maximum 704 in² in listed and labeled kit for positive pressure applications using listed glazing. Minimum 5” from top or edge of door to lite cutout and minimum 5” from latch cutout to lite cutout.
			2. Maximum 32” high.
			3. Maximum 22” wide.
			4. Multiple lights are allowed when the sum of the areas does not exceed the tested area with the maximum length and width limitations.
		5. 20 to 45-minute rated doors.
			1. Listed metal vison frames and listed glazing are limited to a maximum clear view area of 616 in² per lite with a maximum of 1232 in². Lite kits exceeding 100 in² void the temperature requirements per NFPA 80 unless temperature resistive glazing is used.
	2. Louvers.
		1. Listed and labeled louvers.
		2. Maximum 576 in².
		3. Maximum width 24”.
		4. Maximum height 24”.
	3. Hardware.
		1. All hardware must be listed and labeled for use in mineral core fire doors.
		2. Pre-machine doors in accordance with templates from specified hardware manufactures and hardware schedule.
		3. Factory install hardware.
		4. EPT Units
			1. Allowed between top and middle hinge locations.
			2. 1/16” maximum clearance per side when installing EPT.
			3. Limited to maximum 60 min positive and neutral pressure applications.
			4. Intumescent caulk or strips are required on bottom, top, and side of EPT device.
		5. Hardware Schedule.
			1. Choose an item.
				1. Hinges Per NFPA 80, Table 6.4.3.1.

Choose an item. Click or tap here to enter text.

* + - * 1. Locking Hardware

Single point latching on singles, 4-point latching for pairs.

Must be listed for use with mineral-core fire doors.

3-point latching for 60 min and lower pairs with rated astragal.

Surface vertical rods less bottom rod allowed for 45 min or lower singles and pairs with door to door or door to floor fire pin installed in each leaf.

Rim x Rim with listed mullion allowed for 90-min pairs.

Click or tap here to enter text.

* + - * 1. Surface Bolts.

Click or tap here to enter text.

* + - * 1. Protection plates.

Brass, bronze, steel, aluminum, polycarbonate or decorative laminate maximum 12 from bottom rail.

Click or tap here to enter text.

* + - * 1. Astragal

Rated metal astragal required on pairs with 3-point latching, maximum 60 min. duration.

* 1. Wire Raceway
		1. Single swing applications only.
		2. 3/8” x 3/8” bore.
		3. Maximum height of 40” from bottom edge of door.

**PART 3 EXECUTION**

1. **EXAMINATION**
	1. Examine areas to receive doors.
	2. Notify architect of conditions that would adversely affect installation or subsequent use.
	3. Do no proceed with installation until unsatisfactory conditions are corrected.
2. **PREPARATION**
	1. Ensure openings to receive frames are plumb, level, square, and in tolerance.
3. **ERECTION**
	1. Install doors in accordance with manufacturer’s instructions.
	2. Install doors plumb, level, square, true to line, and without warp or rack.
	3. Anchor frames securely in place.
	4. Separate aluminum from other metal surfaces with bituminous coatings or other means approved by architect.
	5. Set thresholds in bed of mastic and back seal.
	6. Install exterior doors to be weathertight in closed position.
	7. Repair minor damages to finish in accordance with manufacturer’s instructions and as approved by architect.
	8. Remove and replace damaged components that cannot be successfully repaired as determined by architect.
4. **FIELD QUALITY CONTROL**
	1. Manufacture’s Field Services.
		1. Manufacturer’s representative shall provide technical assistance and guidance for installation of doors.
5. **ADJUSTING**
	1. Adjust doors, hinges, and locksets for smooth operation without binding.
6. **CLEANING**
	1. Clean doors promptly after installation in accordance with manufacturer’s instructions.
	2. Do not use harsh cleaning materials or methods that would damage finish.
7. **PROTECTION**
	1. Protect installed doors to ensure that, except for normal weathering, doors will be without damage or deterioration at time of substantial completion.

**END OF SECTION**